PRODUCT INFORMATION

PRODUCT CODE: 150 µ WHITE SOFT PVC STATIC LABEL

| PRODUCT CODE |  | 150 µ WHIT SOFT PVC STATIC LABEL |  |  |
| --- | --- | --- | --- | --- |
|  |  |  |  | Surface material |  |  |
| PRODUCT CONSTRUCTION |  | Pressure Sensitive adhesive |  |
|  |  |  |  | Liner |  |  |
| SURFACE |  |  | LINER |  |  |
| ARTICLE NAME |  | SOFT POLYVINYL | ARTICLE NAME | PE LAMI RELEASE PAPER |
|  |  | CHLORIDE |  |  |  |  |
| THICKNESS m/m |  | 0.150 ± 0.009 | THICKNESS m/m | 0.185 ± 0.010 |
| BASIC WEIGHT g/m² |  | 180 ± 11 | BASIC WEIGHT g/m² | 183 ± 10 |
| COLOR |  | WHITE |  | COLOR | WHITE |
| SMOOTHNESS |  | GOOD | SMOOTHNESS | GOOD |
| PRINTABILITY |  | GOOD | DIE CUTTING | GOOD |
|  |  | PRESSURE SENSITIVE ADHESIVE |  |  |
| ADHESIVE BASE |  | - | PEEL ADHESION 180º Kg/25mm² | - |
| COATING THICKNESS |  | - | RELEASE FORCE gm/25mm | - |
| COATING WEIGHT gm/m² |  | - | HOLDING POWER (HR/KG X 25 mm ²) | - |
| SOLVENT RETENTION % |  | - | TEMPERATURE RANGE ºC | 10 ~ 70 |
|  |  |  | TEMPERATURE RANGE ºC | 10 ~ 40 |
| INITIAL TACK NO/ BALL |  | - |  | SHELF LIFE | ONE YEAR |

STOCK ENVIROMENT 30 ºC X 50% RH↓ IN COOL DRY PLACEKEEP AWAY FROM DIRECT SUN LIGHT AND HEAT